User Guide

Mineralogical quantification by mass balance and

calculation of equivalent dissolution depth

Table of Contents

1.	Tool overview	3

1.1 General description	3

1.2 Requirements and installation	3

2.	Mathematical model	3

2.1 Oxide → mineral mass balance	3

2.1.1 Structural formula → oxide composition conversion	4

2.1.2 NNLS algorithm (coordinate descent)	5

2.1.3 Normative mode (greedy selection)	5

2.2 Equivalent dissolution depth	5

3.	Step-by-step interface guide	7

3.1 Step 1: Mineralogical quantification	7

3.1.1 Oxide wt% input	7

3.1.2 Mineral library	7

3.1.3 Phase selection for fitting	8

3.1.4 Running the calculation and reading results	10

3.2 Step 2: Dissolution depth	10

3.2.1 Source of mineralogical proportions	10

3.2.2 Sample geometric and physical parameters	10

3.2.3 Dissolved cation concentrations	11

3.2.4 Results	11

3.3 CSV export	11

4.	Limitations and usage precautions	12

4.1 Mass balance constraints	12

4.2 Depth calculation assumptions	12

4.3 Recommended validation	12

# Tool overview

## 1.1 General description

This Python/Tkinter tool is designed for two complementary tasks in mineralogical geochemistry:

- Step 1: Quantify the mineral phases of a rock or material from its bulk chemistry expressed as oxide wt%, by solving a non-negative constrained mass balance (NNLS). Two solving modes are available: Best Fit and Normative.

- Step 2: Estimate the equivalent dissolution depth of a target mineral phase from the concentrations of cations released into solution during a dissolution experiment.

The two steps are linked: Step 1 results transfer directly to Step 2, but each step can also be used independently.

## 1.2 Requirements and installation

The tool is a standalone Python script. Required dependencies are:

| Library | Minimum version | Usage |
| --- | --- | --- |
| Python | 3.8 | Core language |
| tkinter | inclus (stdlib) | Graphical interface |
| numpy | 1.20 | Linear algebra (NNLS) |
| matplotlib | 3.4 | Oxide exp. vs model plot |
| csv, re, math | stdlib | Read/write, parsing |

Launch the interface:

python mineral_mass_balance.py

# Mathematical model

## 2.1 Oxide → mineral mass balance

The measured bulk chemistry (oxide wt%) is modelled as a linear combination of the oxide compositions of the pure mineral phases. Let:

- b ∈ ℝm: vector of observed oxide contents (normalised to 100 %),

- A ∈ ℝm n: matrix whose jth column is the oxide composition of mineral j (computed from its structural formula),

- x ∈ ℝn: vector of phase mass fractions to be determined.

- W: diagonal weighting matrix

The problem to solve is:

min ‖ A x − b ‖²   subject to   xⱼ ≥ 0  ∀j

The non-negativity constraint is physically motivated: a mass fraction cannot be negative. The solver is a coordinate-descent NNLS.

### 2.1.1 Structural formula → oxide composition conversion

For each mineral phase defined by its structural formula (e.g. Si2.88Al2.63Fe3.08Mg0.95O18H6 for a chlorite), the composition is expressed in normative oxide wt% as follows:

1.	Count atoms of each element i in the formula → nᵢ

2.	Map element → reference oxide (e.g. Fe → Fe₂O₃) and compute moles of oxide: nox=nistoichiométrie_élément_dans_l oxyde

3.	Masse de chaque oxyde : mox=nox×Mox (IUPAC molar masses, 2021)

4.	Normalise to 100 wt%:  wt%ox=moxmox×100

The element → oxide mapping used is:

| Element | Normative oxide | Metal atoms per oxide unit |
| --- | --- | --- |
| Si | SiO₂ | 1 |
| Al | Al₂O₃ | 2 |
| Fe | Fe₂O₃ | 2 |
| Mg | MgO | 1 |
| Na | Na₂O | 2 |
| K | K₂O | 2 |
| Ca | CaO | 1 |
| Ti | TiO₂ | 1 |
| Ba | BaO | 1 |
| Mn | MnO | 1 |
| P | P₂O₅ | 2 |

Note: All iron is assigned to Fe₂O₃ (normative Fe³⁺ convention). The actual iron valence in each mineral is encoded in its structural formula (e.g. Fe3.08 in a reduced chlorite). If the rock contains significant FeO, a prior Fe²⁺/Fe³⁺ correction is required before input.

### 2.1.2 NNLS algorithm (coordinate descent)

The Non-Negative Least Squares (NNLS) algorithm implemented is a projected coordinate descent, also known as the coordinate-wise Lawson-Hanson method. For each variable xⱼ, the one-dimensional subproblem is solved analytically and the result is projected onto ℝ⁺:

xⱼ ← max(0,  xⱼ + (aⱼᵀ rⱼ) / ‖aⱼ‖²)     with rⱼ = b − A x (current residual)

The algorithm converges when ‖x_new − x_old‖₁ < 10⁻⁹ or after 2000 iterations. The solution is then renormalised to 100 %.

Fit quality is assessed by the root mean square error (RMSE) over oxides, expressed in wt%:

RMSE = sqrt( (1/m) Σᵢ (bᵢ − (Ax)ᵢ)² )

Note: An RMSE < 1 wt% is generally satisfactory. High residuals on SiO₂ or Al₂O₃ indicate a missing phase in the library or an incorrect formula. Also check oxide chemistry consistency (total ~ 100 %).

### 2.1.3 Mode Normative (greedy selection)

In Normative mode, phases are selected one by one by a greedy algorithm minimising the RMSE at each step. Only phases that improve the fit beyond the RMSE threshold are retained. Phases with a forced order are injected first in the sequence.

## 2.2 Equivalent dissolution depth

The dissolution depth is estimated from the ratio between the quantity of cation actually released into solution and the total quantity available in the target mineral phase, expressed as a length by analogy with surface dissolution.

For a mineral phase j containing tracer element E with stoichiometry νᴱ (number of E atoms per formula unit):

n_phase = (wt%_j / 100) × m_bulk / M_j

n_E_total = n_phase × νᴱ

depth (µm) = (n_E_solution / n_E_total) × thickness (mm) × 1000

Where:

- mbulk= ρbulk×π×(d2)²×t  [total sample mass in g]

- Mj  = molar mass of phase j [g/mol], computed from its structural formula

- nE_solution  = moles of E measured in the leachate [mol]

- thickness  = sample thickness [mm]

The result represents the thickness of pure phase that would have to be uniformly dissolved to yield the cation amount measured in solution. It is a lower bound if dissolution is heterogeneous or if other phases contribute to the same element.

Note: The phases currently handled are analcime (Na tracer) and chlorites (Mg and Fe tracers). Extension to other phases requires modifying the compute_depths_um() function in the source code.

# Step-by-step pas de l'interface

## 3.1 Step 1 : Quantification mineralogical

### 3.1.1 Oxide wt% des % massiques d'oxydes

The « Add custom oxide... » button opens a dialogue. Fill in:

- Oxide formula (ex. ZrO₂)

- Element symbol (ex. Zr)

- Number of metal atoms dans l'oxyde

- Atomic weight (leave blank if element already in the standard table)

- Initial value en wt%

Note: The added oxide is immediately available in the input fields and can be exported/imported via CSV for later reloading.

| Field | Unit | Description |
| --- | --- | --- |
| SiO₂ … P₂O₅ | wt% | Eleven major oxides. Leave at 0 if not measured. |
| Auto-renormalise to 100 % |  | If checked, input values are normalised before calculation. Recommended if the total deviates from 100 %. |
| Somme (indicateur) | wt% | Displayed in green if ≈ 100 %, red otherwise. |
| Add custom oxide... |  | Dialogue permettant d'ajouter un oxyde hors des 11 standards (ex. ZrO₂). |

### 3.1.2 Mineral library

The text area (labelled « 2) Mineral library ») defines the set of candidate phases. Each line describes a mineral using the syntax:

NomPhase = ElemStoechio  ElemStoechio  ...

- Stoichiometric coefficients are real numbers (decimals allowed).

- O and H are accepted in the formula but do not enter the oxide mass balance.

- Empty lines or lines without « = » are ignored.

Library visual indicators:

| Background colour | Meaning |
| --- | --- |
| Light green | Valid library: N phases loaded successfully |
| Yellow | Library modified and not validated: click Refresh |
| Beige/white | Initial unverified state |
| Light red | No valid phase: check syntax |

Predefined phases (combo):

A drop-down selector offers around twenty common minerals (kaolinite, illite, feldspars, pyroxenes, etc.). Select a mineral and click « Add to library » to append it to the list.

### 3.1.3 Phase selection for fitting

The « 3) Minerals used in fit » panel controls which phases enter the calculation, the solving mode, and weighting.

Mode de fit :

| Mode | Behaviour | Recommended use |
| --- | --- | --- |
| Best Fit | Classic NNLS on all checked phases. All phases can have a non-zero proportion. | Initial exploration, maximise fit quality. |
| Normative | Greedy selection: phases are added one by one as long as they improve the RMSE beyond the set threshold. Yields a parsimonious mineralogical assemblage. | Constrain the number of active phases, normative approach. |

Seuil RMSE Normative :

Visible only in Normative mode. Value in wt% below which adding a further phase is no longer accepted. Default: 0.05 wt%.

Colonne Fixe (wt%) :

Enter a numeric value in the blue field to the right of a phase to fix it at that proportion. Fixed phases are subtracted from the balance before free-phase optimisation. They appear in bleu in the results with flag « F ».

Colonne Ordre (mode Normative uniquement) :

In Normative mode, enter an integer ≥ 1 to force a phase to be injected first in the greedy sequence, ahead of freely selected phases. Useful for imposing mineralogically certain phases (e.g. hematite confirmed by XRD).

Weighting:

| Option | Weight wᵢ | Effect |
| --- | --- | --- |
| None (default) | 1 | Minimise l'erreur absolue. SiO₂ domine l'optimisation. |
| Relative (1/b) | 1/bᵢ | TiO₂ at 1 % counts as much as SiO₂ at 50 %. Recommended for trace oxides. |
| Square root (1/sqrt(b)) | 1/√bᵢ | Compromise: attenuates major oxides without over-amplifying traces. |
| Analytical (1/sigma) | 1/σᵢ | Classic chi². Sigma input fields appear for each oxide. Oxides without a sigma value automatically use 1/b. |

Autres boutons :

- Refresh: re-reads the library and updates the phase list (checked states preserved if the name is unchanged).

- Check all / Uncheck all: global toggle.

- View phases: popup displaying, for each phase, its structural formula and computed oxide composition (normative wt%). Useful for checking formula consistency.

### 3.1.4 Lancement du calcul et lecture of results

Click « Compute mineral wt% ». The status bar displays the final RMSE.

Three result panels are updated:

| Panel | Content |
| --- | --- |
| Results: mineral wt% | Mass fractions of each phase (sorted in descending order). Phases at 0.000 % did not contribute to the fit. |
| Residuals per oxide (Obs - Calc) | For each oxide: observed value, calculated value, absolute residual and relative error. Allows poorly reproduced oxides to be identified. |
| % oxide experimental vs model | Linear (or log) plot overlaying observed and calculated values for visual assessment of fit quality. |

## 3.2 Step 2: Dissolution depth

### 3.1.1 Source des proportions mineralogicals

Two modes are available:

- « Use Step 1 results »: previously computed wt% are reused directly. A summary of the values appears below the radio buttons.

- « Enter mineral wt% manually »: an input field appears for each phase in the library.

### 3.2.2 Sample geometric and physical parameters

| Parameter | Unit | Description |
| --- | --- | --- |
| Thickness | mm | Thickness of the pellet or core used in leaching. |
| Dry bulk density | g/cm³ | Dry apparent density of the sample (unsaturated). Used to compute bulk mass. |
| Diameter | cm | Sample diameter (circular cross-section assumed). |

Note: The code assumes a cylindrical sample. For a different geometry, modify compute_depths_um() in the source code.

### 3.1.3 Concentrations en cations dissous

Enter the total amounts (in mol) of each cation measured in the leachate at the end of the experiment:

| Cation | Traced phase |
| --- | --- |
| Al | Not used in current depth calculations (reserved) |
| Si | Not used in current depth calculations (reserved) |
| Na | Analcime (all variants whose name contains "analcime") |
| Mg | Chlorite (all variants whose name contains "chlorite") |
| Fe | Chlorite (all variants whose name contains "chlorite") |

Note: Phase detection uses a case-insensitive substring search on the phase name. Name chlorites with the word "chlorite" and analcimes with "analcime" to ensure they are picked up.

### 3.2.4 Results

Click « Compute depths ». The table lists, for each detected (phase, tracer) pair, the equivalent dissolution depth in µm.

## 3.3 CSV export

The « Export CSV » button (Step 1) generates a semicolon-delimited file containing:

- Mineral wt% with the structural formula of each phase.

- The oxide residuals table.

- Dissolution depths if they have been calculated.

The file can be opened directly in Excel (via Data → From Text/CSV with « ; » as delimiter).

# Limites and usage precautions

## 4.1 Mass balance constraints

- Under-determination: if n (number of phases) > m (number of oxides = 11), the system is under-constrained. The NNLS will always find a solution, but it may not be unique. Restrict the library to mineralogically plausible phases.

- Iso-chemical phases: two phases very close in composition (e.g. reduced vs oxidised Fe-chlorite) may be difficult to discriminate by mass balance alone. Prefer an external constraint (SEM-EDS analyses, for example) to fix one of them.

- Phases not covered by the 11 oxides: elements such as U, REE, Zr, etc. are not included in the balance. Their contribution remains in the residuals without affecting the solution.

## 4.2 Depth calculation assumptions

- Homogeneous distribution: the calculation assumes the mineral phase is uniformly distributed throughout the sample volume.

- Dissolution congruent dissolution: the leachate composition reflects that of the dissolving phase. Incongruent dissolution (preferential element release, secondary precipitation) is not accounted for.

- No cross-phase contribution: if several phases carry the same tracer element (e.g. Fe in chlorite and haematite), the calculation assigns all Fe to chlorite.

## 4.3 Validation recommended

- Check mineralogical consistency with XRD (at minimum semi-quantitatively).

- Compare RMSE values for different sets of candidate phases.

- Test the sensitivity of computed depths to uncertainties in mineral wt% (vary by ± 2–3 wt% per phase).